# PCB Handling Rack Material Specifications

## Karry-Alls, Angle Racks and RA-18 Rack-All

### February 2002

| ELECTRICAL: | SPECIFICATIONS | ASTM TEST |
| --- | --- | --- |
| Volume Resistivity, ohm-cm, range | 101 - 103 | D-257 |
| Surface Resistivity, ohms/sq, range | 104 - 106 | D-257 |
| Static Decay |  |  |
| Mil B-81705B, 2.0 SEC | Pass | FTMS-4046 |
| NFPA Code 56A, 0.5 SEC | Pass | FTMS-4046 |
| THERMAL: |  |  |
| Deflection Temperature, ºF@264 PSI | 170 | D-648 |
| Deflection Temperature, ºF@ 66 PSI | 260 | D-648 |
| PERMANENCE: |  |  |
| Specific Gravity | 1.20 | D-792 |
| Water Adsorption | 0.01 | D-750 |
| MECHANICAL: |  |  |
| Impact Strength, IZOD, notched 1/8”, FT-LB/IN | 0.50 | D-256 |
| Tensile Strength, PSI | 3,200 | D-638 |
| Tensile Elongation, % | 6-8 | D-638 |
| Tensile Modulus, PSI x 106 | 0.50 | D-638 |
| Flexural Strength, PSI | 5,500 | D-790 |
| Flexural Modulus, PSI x 106 | 0.40 | D-790 |
| FLAMMABILITY: |  |  |
| Coefficient of Linear Therman Expansion, IN/IN/ºFx105 | 3.0 | D-696 |

###### RA-20 CP MATERIAL SPECIFICATION

| ##### MECHANICAL PROPERTIES: * | Unit | ASTM Test | PP-62/EC/H |
| --- | --- | --- | --- |
| Tensile Strength | PSI | D638 | 3,700 |
| Elongation | % | D638 | 10 |
| Izod Impact (1/8’) | FT-LBS/IN | D256 | 6.0 |
| ##### PHYSICAL PROPERTIES: |  |  |  |
| Specific Gravity | - | D792 | 0.98 |
| ##### THERMAL PROPERTIES: |  |  |  |
| Deflection Temp. Under Load | ºF | D648 | 125 |
| ##### ELECTRICAL PROPERTIES: |  |  |  |
| Surface Resistivity | OHMS/SQ | D257 | 104 - 108 |
| *All Mechanical tests conducted at 73º unless otherwise noted. IEE-022 |  |  |  |