| TONNAGE CALCULATION |  |
| --- | --- |
| Use the guidelines below to calculate the needed tonnage for your stamping project. |  |
| # General Formula for Press Tonnage Required |  |
| Determine the approximate press tonnage needed to stamp a part based on linear inches of cut. |  |
| For Steel: Material Thickness X Inches of Cut x 25 = Press Tonnage |  |
| Example: |  |
| Need: 2” Square washer from .088 thick steel |  |
| Base Material: 2 –1/2” coil X 2-1/2” progression |  |
| 1” O 2” 2” |  |
| Calculation: 2 + 2 + 2 + 2 = 8 |  |
| 1” circle perimeter ( II D ) 3.14 X 1” = 3.14” |  |
| Total Inches of Cut = 8 + 3.14 = 11.14 |  |
| Tonnage Required: |  |
| .088 Thick X 11.14 X .25 (factor) = 24.5 tons |  |
| Blanking or Perforating Pressures: |  |
| Blanking or Perforating pressure (in tons) equals the total length of cut, or cuts, be it portions or the entire circumference of a circle, the sum of a square, rectangle, or triangle, or the entire total circumference of a number of holes multiplied by the material thickness, multiplied by the shearing strength of material. For answer in tons, the shearing strength must be converted from pounds/square inch (PSI) into tons/square inch by dividing by 2000. |  |
| Example: |  |
| Mild steel (shearing strength) = 50,000 PSI/2000 = 25 tons/square inch |  |
| For drawing, use same method except use tensile strength of material. |  |